Course help - David Moore - 01626 331351 - dcmoore@timber.org.uk

AN ANSWER TO ROT
Exercise 2

·  You are standing inside a roof with the following tools: a torch, a tape measure, a 'damp' testing meter, a screwdriver, plus a pad and pencil.

(Use the attached form to make notes as you go and then compare them with the suggested answers).

What you can see

Sloping timbers (common rafters) coming down from the top (ridge) to sit at the bottom on the wall. They are sitting on another piece of wood which is a horizontal beam across the building (tie beam or collar).

Checking for defects

You notice that the Tie Beam looks creased and darkened at the end where it sits on the wall.

Q.  What other symptoms of decay or attack might you notice?

A. Mould (white), splitting or cracking (into cubes), insect holes of various sizes, sagging of the roof, smell, nests, Bat droppings, Rat droppings, strands, mushrooms or ‘skins’ (mycelium) of Dry or Wet rot.

Q. Would these differ at all if the roof was made of a softwood (Pine) or a hardwood (say, Oak)?

A. Yes. Hardwoods are more resistant to attack for longer than softwoods, but when wet enough are attacked by Death Watch Beetle: this beetle makes larger holes than Common Furniture beetle and does more damage, especially up the centre of the bearing ends.

Look for the cause

Q. What is causing the creasing and darkening?

A. Water getting in somewhere, causing rot (creasing, shrinkage)

Q. How are you going to confirm that the cause is still present?

A. Use the ‘moisture meter’ but check it is calibrated for timber first.

Q. Suggest the 'moisture meter' readings on which you might advise a Client as follows: a)no action required, b)at risk, needs treatment

A. a) below 16%  b) above 18% up to saturation at 28-32%

Q. Give as many examples as possible of where could the cause be coming from?

A. Roof leak from slates/tiles/felt/chimney flashing, Water leak from pipe, tank, gutter, valley, Penetrating damp from gable wall, poor pointing, missing bricks, cracked render, Condensation from poor ventilation, uncovered water tank, living space use, non-breathing felt, over-stuffed eaves (insulation), over-insulated ceilings, Fire Damage from Fire Service use of water, Bird nesting causing bulges in the felt, Rat Infestation causing damage to felt.

Assess the damage

Q. How would you decide to what depth the timber is damaged?

A. Use your screw driver. For cracks or splits gauge the depth with a piece of paper or your pencil.

Q. Approximately what proportion of the timber can be damaged and surface repaired, without needing to cut out the section?

A. Up to a maximum of one third of the cross sectional area, unless a Structural Engineer says otherwise. Some defects are more serious than others.

Q. Is damage more important in one part of the timber than another, from a structural point of view?

A. Yes, the mid span of the Tie Beam carries the largest bending load and because timber bends by compressing the upper half and stretching the lower half, so damage in the upper half is easier and safer to repair. Damage in the lower half usually needs rods to be embedded in order to resist the stretching or tension.

Also, the bearing end of the Tie Beam should be fixed to the Rafter and/or wall plate to resist the weight of the roof (particularly with snow on it) from moving down and out – spreading. If the Tie Beam and/or Rafter feet are badly rotted the roof could, in theory, collapse. This ‘spreading’ load is also, in some roof designs, resisted by the addition of other timbers – horizontal ‘ties’ or ‘collars’ above ceiling level.  Sometimes people remove them, to allow the roof to be used as an attic space. Lack of connection, due to decay or splitting, can cause dangerous movement. Always recommend a Structural Engineer if you see any signs of structural alteration or movement.

Offer a repair

In one area there is slight surface damage: when dug out the missing wood measures 1 inch (25mm) x 2 inches (50mm) x 4 inches (100mm).

Q.  What volume in cc's or litres of repair product will you need and what type of product could you use?

A. 125cc or 0.125 litres (just over an eighth of a litre).

The bottom 3 foot 3 inches (1 metre) of the 12 inch (300mm) x 10 inch (250mm) Tie Beam is beyond repair.

Q. Which timber repair technique could you use to replace it?

A. Timber-Resin Splice – use a Type C for a Top Slot fixing, with top slots being cut on site, most commonly used where the roof coverings are left in-situ. Or you could use a Type E where holes are drilled on site and the new timber part (the TRS) comes with the slots built in.

Q. Which types of resin products are you likely to use?

A. For Top Slot repairs a Quick Setting Polyester Paste is used for the face joint. The Structural Resin is a Structural Epoxy Pouring Grout, poured directly into the slot(s).

Q. What techniques could be used to cut slots or holes into the remaining timber, for connection to a new piece?

A. Slots can be cut with an Auger or 3D Cutter in an electric drilling machine, with a chain saw or a slot cutting saw, using a chisel to clean out the roughed out slot.

Q. How much do you think the repair materials would cost?

A. For a 12 x 10 inch timber x 1 metre cut off made in softwood about £500.00.

Q. How long do you think it would take one man to cut out and replace one Tie Beam end, assuming the Rafter foot was sound?

A. Excluding travel, access, propping and making good about 4 hours.

Q. What types of treatment could you offer, to minimise the risk of future rot?

A. After repair, surface treat with Boron Gel to at least 300mm (12 inches) clear of all dampness (meter readings over 16%): if Dry Rot has been found also drill and inject Boron Paste.

Q. What other measures might you take, depending on the type of roof coverings, to reduce the risk of mould growth and insect attack?

A. Increase ventilation (eaves vents, roof vents), check stored goods for old timbers, furniture etc that might be infested, advise the client about checking for future water leaks, ingress of snow, rats and birds.

Course  help - David Moore - 01626 331351 - dcmoore@timber.org.uk

Site: ©1998 D C Moore
Page Design:- dcmoore@timber.org.uk